“This document is the Accepted Manuscript version of a Published Work that appeared in final form in ACS Nano, 2021, 15, 1548-1554 copyright © American Chemical Society after peer review and technical editing by the publisher. To access the final edited and published work see doi:10.1021/acsnano.0c08995”

On-Surface Synthesis and Intermolecular Cycloadditions of Indacenoditetracenes, Antiaromatic Analogues of Undecacene

Rafal Zuzak,† Otilia Stoica,‡,∥ Rémi Blieck,‡ Antonio M. Echavarren,‡,∥,* Szymon Godlewski†,*

†Centre for Nanometer-Scale Science and Advanced Materials, NANOSAM, Faculty of Physics, Astronomy and Applied Computer Science, Jagiellonian University, Łojasiewicza 11, PL 30-348 Krakow, Poland

‡Institute of Chemical Research of Catalonia (ICIQ), Barcelona Institute of Science and Technology, Avenida Països Catalans 16, 43007 Tarragona, Spain

∥Departament de Química Orgànica i Analítica, Universitat Rovira i Virgili, C/Marcel·lí Domingo s/n, 43007 Tarragona, Spain

ABSTRACT: The formation of s-indaceno[1,2-b:5,6-b']ditetracene and as-indaceno[2,3-b:6,7-b']ditetracene containing indenofluorene cores from a common precursor has been achieved by a dehydrogenative surface-assisted cyclization on Au(111) and confirmed by bond-resolved non-contact atomic force microscopy. On-surface generated as-indaceno[2,3-b:6,7-b']ditetracenes undergo fusion, which leads to a T-shaped adduct by an intermolecular cycloaddition. The same type of cycloaddition, which has no parallel in solution chemistry, has been observed between as-indaceno[2,3-b:6,7-b']ditetracene and pentacene or octacene. These examples of surface-assisted cycloaddition provide perspectives for the rational design and synthesis of molecular nanostructures.

KEYWORDS: on-surface synthesis, cycloadditions, indacenoditetracene, antiaromatics, cyclodehydrogenation

Acenes are a family of linearly fused polycyclic aromatic hydrocarbons (PAHs) whose band gap and reorganization energies were predicted to diminish as a function of their length. [1-4] This behavior was later demonstrated experimentally by the steady decrease of the HOMO-LUMO gap from 2.2 eV in pentacene [5] to approximately 1.1-1.2 eV for decacene and undecacene. [6-8] However, the trend was broken by the discovery that for dodecacene, the largest member of the acene family characterized up to now, the energy gap increases up to 1.4 eV, as a possible result of its higher polyradical character. [9]

The s-indaceno[1,2-b:5,6-b']ditetracene (1) and as-indaceno[2,3-b:6,7-b']ditetracene (2) are analogues of undecacene bearing two five-membered rings (Figure 1a). Indacenoditetracenes 1 and 2 are interesting targets as they have embedded indeno[1,2-b]fluorene (3) [10-12] and indeno[2,1-a]fluorene (4) [13-14] substructures, which have been reported to have partial diradicaloid character. [15-16] However, it has been recently reported that the paratropicity of s-indacenes decreases when the terminal acene parts are extended. [17-19] Molecules with embedded indenofluorene units generated through surface-assisted synthesis have attracted recent interest as advanced materials with intriguing electronic properties. [20-22] Interestingly, PAH 5, a benzo-analogue of 4, has been reported to react in Diels-Alder reactions at the internal 4b/8b positions, [14] presumably as a result of the substitution at positions 13/14 by bulky 2,4,6-trimethylphenyl (mesityl) groups (Figure 1b).

Most of the carbon-carbon bond formation reactions in the field of on-surface synthesis involve dehalogenative or dehydrogenative couplings, as well as simple condensation reactions, [23-25] although a few examples of formal [2+2] cycloadditions have also been reported. [26-27] Very recently the dehydro-Diels-Alder reaction has been applied for the on-surface construction of diverse PAHs from dibromo-bis(phenylethynyl)benzene on the Au(111) surface. [28-29]

We report here the formation of 1 and 2 from a common precursor 11a by a combination of our gold(I)-catalyzed cycloaddition approach, followed by an on-surface dehydrogenative cyclization. Surprisingly, we have found that on-surface generated as-indaceno[2,3-b:6,7-b']ditetracene (2) reacts through its ortho‐quinodimethane [30] central part with acenes to form extended PAHs 7 with an indeno[1,2,3-cd]fluoranthene substructure (Figure 1c).

The high reactivity and insolubility of unsubstituted acenes larger than pentacene is a barrier for their synthesis under conventional in-solution conditions, which has been circumvented by the use of on-surface synthesis. [6,7,9,23,31-33] In this context, we have recently developed a synthesis of long acenes by first preparing partially saturated acene derivatives (hydroacenes) using a gold(I)-catalyzed formal [4+2] cycloaddition, [34] followed by dehydrogenation on a metal surface. [7,35,36] This approach allowed us to use not only pentacene, but also octacene as a component in the surface-assisted cycloaddition with 2.

Figure 1. (a) Structures of s-indaceno[1,2-b:5,6-b']ditetracene (1), as-indaceno[2,3-b:6,7-b']ditetracene (2), and the parents indeno[1,2-b]fluorene (3) and indeno[2,1-a]fluorene (4). (b) Diels-Alder cycloaddition of 5 to form 6.14 (c) Formal cycloaddition of 2 with acenes to form T shaped molecules 7.

Scheme 1. Synthesis of 1 and 2 via gold(I)-catalyzed [4+2] cycloaddition and on surface dehydrogenative cyclization.

RESULTS AND DISCUSSION

Synthesis of precursors. The synthesis of 1 and 2 started by the Sonogashira coupling of diiodoterphenyl 8 [37] with previously reported 1,7-enyne 9 [34] to give 10, which was followed by a double gold(I)-catalyzed [4+2] cycloaddition, [7,34] giving rise to 11a (Scheme 1). [38]

On-surface synthesis of indacenoditetracenes. After deposition of 11a at room temperature on Au(111) and annealing at 370 °C the resulting cyclized molecules 1 and 2 are found separate and located within the surface reconstruction pattern elbows, being the most reactive areas of the Au(111) surface with undercoordinated gold atoms (Figure 2a). Such preferred localization of organic molecules has been already frequently reported in the past. [7,35,39] While the majority of the molecules could be found as isolated entities (approximately 63±7 %), the presence of larger and differently shaped features suggests either self-assembling or intermolecular reactions. Although the annealing temperature is too low for cross-coupling of benzenoid hydrocarbons, the anticipated formation of more reactive pentagonal rings makes such processes reasonable. Further information could be grabbed from the magnification visualized in Figure 2b, where elongated features resembling highly squeezed Z-shape molecules with an exemplary one marked by a dashed green rectangle are present. We have noted that the abundance of such appearing molecular features reaches approximately 63±8 %. Apart from these features - located mainly within surface herringbone pattern elbows and infrequently within the fcc areas – we also observed a few different molecules. Among them, we can distinguish V-shaped features marked for clarity by a white dashed rectangle (approximate abundance of 20±4 %), dome linear objects – highlighted by a yellow dashed rectangle (abundance of 17±4 %) and also larger structures marked by circles and triangles. The limited extension of their STM appearance strongly suggests that they are formed through intermolecular cycloaddition reactions rather than simple self-assembly.

In order to shed more light on the details of the internal structure of observed molecular architectures, we have captured a CO molecule on a microscope tip apex to increase the imaging resolution. [40] In Figure 2c the high-resolution image of the sample is presented. We note here the clearly noticeable highly squeezed Z appearance of the molecules marked again by dashed green rectangles. As already mentioned, these are the most frequently found entities and could be linked with the anticipated generation of the s-indaceno[1,2-b:5,6-b']ditetracene (1) molecules, which structural scheme is marked by a green rectangle in Figure 2d. For clarity the newly on-surface formed bonds are highlighted in purple. Further, within Figure 2c we can distinguish two types of linear structures, which are marked by yellow and light gray rectangles. Both groups of entities exhibit quite uniform STM appearance, hence the high-resolution image allows for clear differentiation between them. We have found that all molecules exhibiting the appearance marked with the yellow dashed rectangle are exclusively located within the surface pattern elbows.  Figure 2. STM images of the molecules after deposition on the Au(111) and annealing at 370 °C; (a) large-scale overview image; (b) filled-state STM image of the area marked in (a) by a white, dashed square, green rectangle marks the exemplary squeezed Z-shape feature, white rectangle shows the V-shaped molecule, yellow rectangle highlights the straight-appearing molecule located within the surface reconstruction pattern corner, white triangle indicates on the T-shape molecular feature, whereas white circle marks the pitch-fork molecule, finally the yellow circle points on the two covalently linked molecules; (c) high resolution empty-state STM image acquired with a CO functionalized tip, the dashed figures mark molecules exactly in the same manner as in (a) and additionally the light gray dashed rectangle indicates the straight – appearing molecule, which is not pinned by the surface reconstruction pattern elbow; (d) structural schemes of the s-indaceno[1,2-b:5,6-b']ditetracene (1) (green rectangle) and as-indaceno[2,3-b:6,7-b']ditetracene (2) (yellow rectangle) with new on-surface generated bonds highlighted in purple, as in Scheme 1; (e) high-resolution STM image, the molecular structures are marked as in (a,b), additionally the three molecules covalently linked into the double T-shape are highlighted by the dashed, white rectangle; (f) high-resolution filled-state STM image obtained with increased precursor coverage with clearly noticeable preferred location of the transformed molecules in the reconstruction pattern corners and the fcc surface areas; scanning parameters: a,f (-1.0 V, 100 pA), c (+0.5 V, 15 pA).

These molecules are characterized by the presence of an additional bump located at one side of the otherwise almost straight and elongated shape of the STM appearance and we have noticed that in all cases the additional bump is located in the vicinity of the vertex of the herringbone pattern. This observation suggests that such appearance might be linked with the interaction between the molecule and the most reactive area of the surface. In contrast, the molecules marked by a light gray rectangle exhibit almost linear appearance without the above described additional lobe (see also Figure S1). Such molecules are exclusively found within the fcc surface areas and are oriented almost perpendicular to the surface herringbone pattern. It is likely that both groups of molecules correspond to as-indaceno[2,3-b:6,7-b']ditetracene (2), generated by the cyclization of 11a at the 2,3-positions (ortho,ortho) of the central benzene ring. However, reaction at the less sterically hindered 2,5-positions would be expected to be favored leading to the formation of 1, which is in perfect agreement with our STM analysis, which points to the more than the three times greater ratio 1 compared to 2.

High resolution STM image shown in Figure 2c enables more detailed analysis of the structures, which we have grouped previously by white and yellow dashed circles. They both correspond to architectures comprised of two molecular precursors, however, we have here distinguished the ones marked with white circles due to their very characteristic appearance, which resembles the shape of the tuning fork. Their appearance suggests their formation from two molecules of 1 cross-coupled along the tetracene moieties of both molecules. The molecular structures marked by yellow dashed circles include the remaining differently shaped covalently bound objects comprised of two transformed precursors, excluding only those marked previously by white circles and triangles (for a magnified image see Figure S1). Here, we can clearly distinguish in Figure 2c structures resulting from the coupling of three units or 1 or 2. Figure 2e focuses on the objects indicated by the white dashed triangles with a characteristic T-shape, which are clearly derived from perpendicular connection of two precursor molecules, as a result of the cycloaddition reaction of 2 through its central o-quinodimethane moiety with the terminal aryl ring of another molecule. As indicated by the white dashed square in Figure 2e, molecules resulting from a combination of three molecules coupled covalently in a perpendicular manner are also formed. Finally, Figure 2f acquired with increased molecule coverage, shows that after passivation of the surface reconstruction elbows, the molecules accumulate preferentially within the fcc areas and that all above described differently shaped groups of molecules could be distinguished. Additionally, we pay attention to the appearance of unstable molecules within fcc or hcp areas. Their instability is manifested by the fuzzy appearance during scanning, this is indicated by white arrows in Figure 2f.

Structure analysis with bond-resolved atomic force microscopy. In order to complement STM measurements and confirm the generation of described molecular nanoarchitectures we applied nc-AFM imaging with CO functionalized tips, which has been established as an ideal tool for single molecule structural analysis by bond resolved images. [41] Firstly, we focus on the molecular objects comprising two covalently merged precursors forming the molecules with a tuning fork shape, whose structure was assigned as 14 (Figure 3). Among other possible pathways, compound 14 could arise by dimerization of two molecules of 9,21-dihydro-s-indaceno[1,2-b:5,6-b’]ditetracene (12), an intermediate in the formation of 1 from 11a, to give 13, followed by the step-wise formation of the four additional C-C bonds (Figure 3c).

Figure 3. Molecular pitch-fork 13 generated from covalent coupling of two precursors; (a) high resolution empty-state STM image, scanning parameters: +0.5 V, 15 pA, (b) frequency shift nc-AFM image; (c) proposed reaction pathway for the formation of 14 by dimerization of 12 via intermediate 13.

The combination of high-resolution STM images with bond-resolved nc-AFM ones for the detailed characterization of the most frequently observed entities is presented in Figure 4. Figures 4a-b show the very same area imaged with the application of high resolution STM and nc-AFM, respectively. We note the presence of the elongated and squeezed Z-like features located within the fcc areas, which are stably visualized in the STM imaging, however, unstable and mobile during nc-AFM, which precludes from their doubtless and detailed characterization. Having in mind the previously described stability of the molecules localized within the surface reconstruction pattern elbows, we have found another molecule exhibiting the squeezed Z-shape and located exactly within the surface ridge corner in order to approach with STM and nc-AFM. The results of the combined measurements are shown in Figures 4c-d presenting the high resolution STM and bond-resolved nc-AFM images, respectively. The images provide doubtless identification of the feature as molecule 1. With that we confirm successful cyclodehydrogenation of 11a to form 1. We indicate here that molecules 1 pinned by the surface reconstruction and stable during STM/nc-AFM imaging may exhibit slightly inclined configuration as visualized by the nc-AFM image shown in Figure 4d, in which one side is displayed as noticeably brighter. In contrast, 1 adsorbed within the fcc surface areas are exhibiting increased instability during STM and especially nc-AFM imaging, as clearly inferred from Figure 4b, showing molecule movement during measurements. However, their appearance in the nc-AFM images may indicate slightly more planar configuration, which is likely correlated with weaker interaction with the underlying substrate.

In order to acquire more information about molecules 1 on Au(111), we performed scanning tunneling spectroscopy measurements. The experiment revealed differences between the molecules located within the fcc areas and those pinned at the surface reconstruction ridge corners. The single point spectroscopy of the former shows clearly resonances at -0.55 V and +1.45 V deriving a gap of approximately 2 eV, as shown in Figure S2. The dI/dV lateral mapping presented in Figure S2 confirms that the above-mentioned STS resonances originate from the molecular states. However, due to the overall instability of the molecule and its tendency to escape away from the STM tip, our attempts for higher spatial resolution failed. The obtained gap value of 2.00 eV is in good agreement with previously reported gas phase calculations for 1, which indicated the gap value of 1.87 eV. [18] Nevertheless our analysis does not account for gap renormalization due to screening effects, which leads to gap shrinking for molecules upon adsorption on metallic surfaces. [42] Furthermore, due to increased reactivity of the pentagonal rings present in the indenofluorene scaffold one may expect hybridization between the molecule orbitals and the surface, as already reported for polycyclic nanostructures with indenofluorene units on Au(111). [20-21] Thus, similar effects are likely to occur also in the case of 1. Interestingly, the data recorded for the more stable molecules pinned by the surface reconstruction pattern elbows exhibits clear differences. Both the single point spectroscopy is characterized by multiple resonances and the spatial mapping shows asymmetric appearance, as indicated in Figure S2, which suggests the increased influence of the substrate on the molecule electronic structure.

Having analyzed the most frequently appearing molecule 1, we characterized in detail the remaining objects shown in Figure 4a-b. In the right-hand lower corner of Figure 4a an almost straight feature with an additional bump is recorded. Corresponding nc-AFM image shown in Figure 4b confirms our previous assignment of this molecule as 2. The bond-resolved nc-AFM image points to the inclination of the central part of the molecule with the phenyl ring protruding from the surface and two pentagonal rings rotated toward the surface within the surface pattern corner. Such configuration could be rationalized by the high reactivity of both the specific surface areas as well as the 1,3-diene moiety located in the central part of the molecule 2. The high resolution STM and corresponding nc-AFM images of such a molecule are shown in Figure 4f-g, respectively. We note here the presence of the very characteristic and intense bright lobe within STM image, which is located in the middle of the molecule length and corresponds to the inclined phenyl ring pointing away from the surface. We could not acquire the nc-AFM image of the less stable configuration of molecule 2 found within the fcc surface area away from the pattern elbows (marked in Figure 2c by the light gray dashed rectangle).

The high resolution STM and corresponding bond-resolved nc-AFM images of the interesting T-shaped molecule, assigned as 15, resulting from covalent merging of two molecular precursors are displayed in Figures 4i-j. Close inspection of the STM appearance of the T-leg indicates on almost identical appearance as for the isolated 2 located in the fcc surface area (Figure S1). Combining this observation with the appearance of the bond-resolved nc-AFM image

Figure 4. Most frequently appearing molecular objects upon deposition of precursors followed by 370 °C annealing; (a) high resolution STM image showing six molecular features; (b) corresponding to (a) frequency shift nc-AFM image, two molecules 1 on the left are instable and mobile during measurement; (c) squeezed Z-shape STM image, corresponding to (c) bond resolved nc-AFM image proving generation of 1, which scheme is displayed in (d); (f) STM image of the straight-appearing 2 pinned by the surface pattern corner, (g) corresponding bond-resolved nc-AFM image showing 2 with clear deviation from flatness, the two pentagonal rings of the conjugated diene moiety are inclined toward the surface leading to out-of-plane configuration of the central phenyl ring, (h) shows the structural scheme of 2; (i) and (j) display the STM and bond resolved nc-AFM images of the T-shape molecular nanostructure 15, respectively, proving generation of the additional phenyl ring between the covalently linked molecules 2, which adopt planar flat-lying configuration, the structural image of the observed object is visualized in (k), the new intramolecular bonds are highlighted in red, while the intermolecular bonds formed during on-surface reactions are marked in green; (l) and (m) STM and nc-AFM images of the V-shaped molecule 16, respectively; (n) structural scheme corresponding to the molecule shown in (l, m); scanning parameters of STM images: +0.5 V, 15pA.

of the T-leg, which clearly demonstrates its formation from 2 exhibiting planar configuration, strongly supports our interpretation of 2 adopting planar configuration, when located away from the reconstruction elbows and less interacting with the surface. Interestingly the appearance of the T molecular unit confirms the cycloaddition between two indacenoditetracene units 2 to form 15 by an on-surface cycloaddition reaction (Figure 4k). This cycloaddition might proceed stepwise by a radical mechanism, and not in the concerted manner of standard Diel-Alder reactions.

Finally, the high resolution STM and nc-AFM images in Figure 4l-m solve the structure of molecules with V-type appearance, which correspond to structure 16 (Figure 4n). This molecule 15 originates from the minor regioisomer 11b formed in the cyclodehydrogenation of precursor 10 (see Supporting Information). [38]

Surface-assisted cycloadditions. The unexpected formation of the T-shaped molecules 15 by on-surface cycloaddition of two molecules of 2 suggests the possibility to perform heteromolecular cycloadditions from two different molecules leading to other types of T-shaped molecular structures. Thus, we tried the reaction with both pentacene and octacene. In the second case, the octacene was generated on the Au(111) surface from tetrahydrooctacene (octacene-H4), according to our original procedure. [7] The 11a precursors were sublimed onto Au(111) and following the above described method, they were transformed into indacenoditetracenes 1 and 2 by 370 °C annealing. Pentacene or octacene-H4 have been deposited subsequently on the same sample followed by the 370 °C annealing in order to initiate heteromolecular cycloaddition. The results are shown in Figure 5. Panels a and b present the high resolution STM and bond resolved nc-AFM images, respectively. They indicate on the successful cycloaddition of pentacene and octacene with 2 to form T-nanostructures 17 and 18, respectively.

Figure 5. Intermolecular fusion between 2 and acenes; (a) and (b) show high resolution STM and bond resolved nc-AFM images of the molecules generated through on-surface fusion of 2 and pentacene, additional pentacene molecule is visualized in the bottom right-hand corner, (c) shows magnified image of the generated T-shape nanoarchitecture; (d) scheme of the on-surface processes leading to the T-shape molecule 17; (e) and (f) display high-resolution STM images of the T-shape nanostructure 18 obtained through covalent merging of 2 with octacene formed from the tetrahydrooctacene precursor; (g) scheme of the processes leading to covalent linkage between 2 and parent octacene; imaging conditions: (a) +0.5 V, 25 pA, (e,f) +0.5 V, 15 pA.

CONCLUSIONS

In summary, we have achieved the on-surface synthesis of s-indaceno[1,2-b:5,6-b']ditetracene and as-indaceno[2,3-b:6,7-b']ditetracene –antiaromatic analogues of undecacene comprising an indenofluorene core - by a dehydrogenative cyclization. Whereas s-indaceno[1,2-b:5,6-b']ditetracene is mainly observed as single entity or engages in intermolecular dimerization leading to larger PAHs, as-indaceno[2,3-b:6,7-b']ditetracene reacts in intermolecular cycloaddition reactions leading to T-shaped nanostructures. We have also observed this type of cycloaddition between as-indaceno[2,3-b:6,7-b']ditetracene and pentacene or octacene, which react at the terminal benzene ring. In the context of on-surface synthesis this unexpected formal cycloaddition reaction provides perspectives for the rational design of complex nanostructures from the appropriate precursors.

METHODS

Experimental Details. All experiments were conducted in the Scienta Omicron STM/nc-AFM microscope in LHe temperature(5 K) with the base pressure in the microscope chamber below 3×10-10 mbar. The Au(111) monocrystalline samples were prepared by the standard procedure of simultaneous annealing and ion sputtering (Ar+ ions). The molecules were evaporated from a Knudsen cell (Kentax GmbH), at the temperature of T = 210 °C (11a), 210 °C (octacene-H4), 130 °C (pentacene). The molecular flux was maintained at the approximate rate of 0.1Hz/min with the application of a quartz microbalane. After deposition, the samples with precursors were annealed at 370 °C by a resistive heater in the preparation chamber (temperature of the sample was monitored by the thermocouple, type K). To obtain high-resolution constant height frequency shift nc-AFM images, the procedure for nc-AFM tip functionalization described by Gross et al. was applied. [41] In all nc-AFM measurements the resonant frequency of the qPlus cantilever was ~26 kHz and the oscillation amplitude kept in the range of 100-150 pm. For image processing Scanning Probe Image Processor and WSxM [43] software has been applied.

ASSOCIATED CONTENT

Supporting Information.

The Supporting Information is available free of charge at https://pubs.acs.org/doi/xxx.

Additional STM images of on-surface generated molecular units; scanning tunneling spectroscopy data for s-indaceno[1,2-b:5,6-b']ditetracene (1); details of molecular precursor synthesis.

Notes

The authors declare no competing financial interest.

AUTHOR INFORMATION

Corresponding Author

E-mail: szymon.godlewski@uj.edu.pl, aechavarren@ICIQ.ES

Author Contributions

The manuscript was written by S.G and A.E. All authors have given approval to the final version of the manuscript.

ACKNOWLEDGMENT

We acknowledge financial support from the National Science Center, Poland (2017/26/E/ST3/00855), ERC Proof of Concept GAP 837225, Ministerio de Ciencia e Innovación (PID2019-104815GB-I00), and the AGAUR (2017 SGR 1257 and FI fellowship to O.S.).

REFERENCES

(1) Anthony, J. E. The Larger Acenes: Versatile Organic Semiconductors. Angew. Chem. Int. Ed. 2008, 47, 452–483.

(2) Bendikov, M.; Wudl, F.; Perepichka, D.F.  Tetrathiafulvalenes, Oligoacenenes, and Their Buckminsterfullerene Derivatives: The Brick and Mortar of Organic Electronics. Chem. Rev. 2004, 104, 4891−4945.

(3) Dorel, R.; Echavarren, A. M. Strategies for the Synthesis of Higher Acenes. Eur. J. Org. Chem. 2017, 14–24.

(4) Dorel, R.; Echavarren, A. M. From Palladium to Gold Catalysis for the Synthesis of Crushed Fullerenes and Acenes. Acc. Chem. Res. 2019, 52, 1812–1823.

(5) Soe, W.-H.; Manzano, C.; De Sarkar, A.; Chandrasekhar, N.; Joachim, C. Direct Observation of Molecular Orbitals of Pentacene Physisorbed on Au(111) by Scanning Tunneling Microscope. Phys. Rev. Lett. 2009, 102, 176102.

(6) Krüger, J.; Eisenhut, F.; Skidin, D.; Lehmann, T.; Ryndyk, D. A.; Cuniberti, G.; García, F.; Alonso, J. M.; Guitián, E.; Pérez, D.; Peña, D.; Trinquier, G.; Malrieu, J.-P.: Moresco, F.; Joachim, C. Electronic Resonances and Gap Stabilization of Higher Acenes on a Gold Surface. ACS Nano 2018, 12, 8506–8511.

(7) Zuzak, R.; Dorel, R.; Kolmer, M.; Szymonski, M.; Godlewski, S.; Echavarren, A. M. Higher Acenes by On-Surface Dehydrogenation: From Heptacene to Undecacene. Angew. Chem. Int. Ed. 2018, 57, 10500–10505.

(8) Shen, B.; Tatchen, J.; Sanchez‐Garcia, E.; Bettinger, H.F. Evolution of the Optical Gap in the Acene Series: Undecacene. Angew. Chem Int. Ed. 2018, 57, 10506–10509.

(9) Eisenhut, F.; Kuhne, T.; García, F.; Fernandez, S.; Guitián, E.; Pérez, D.; Trinquier, G.; Cuniberti, G.; Joachim, C.; Peña, D. Moresco, F. Dodecacene Generated on Surface: Reopening of the Energy Gap. ACS Nano 2020, 14, 1011–1017.

(10) Zhou, Q.; Carroll, P. J.: Swager T. M. Synthesis of Diacetylene Macrocycles Derived from 1,2-Diethynyl Benzene Derivatives: Structure and Reactivity of the Strained Cyclic Dimer. J. Org. Chem. 1994, 59, 1294–1301.

(11) Chase, T.; Rose, B. D.; McClintock, S. P.; Zakharov, L. N.; Haley, M. M. Indeno[1,2‐b]Fluorenes: Fully Conjugated Antiaromatic Analogues of Acenes. Angew. Chem. Int. Ed. 2011, 50, 1127–1130.

(12) Majzik, Z.; Pavliček, N.; Vilas-Varela, M.; Pérez, D.; Moll, N.; Guitián, E.; Meyer, G.; Peña, D.; Gross, L. Studying an Antiaromatic Polycyclic Hydrocarbon Adsorbed on Different Surfaces. Nature Commun. 2018, 9, 1198.

(13) Shimizu, A., Tobe, Y. Indeno[2,1‐a]Fluorene: An Air‐Stable Ortho‐Quinodimethane Derivative. Angew. Chem. Int. Ed. 2011, 50, 6906–6910.

(14) Miyoshi, H.; Nobusue, S.; Shimizu, A.; Hisaki, I.; Miyata, M.; Tobe, Y. Benz[c]indeno[2,1-a]Fluorene: A 2,3-Naphthoquinodimethane Incorporated into a Indenofluorene Frame. Chem. Sci. 2014, 5, 163–168.

(15) Shimizu, A.; Nobusue, S.; Miyoshi, H.; Tobe, Y. Indenofluorene Congeners: Biradicaloids and Beyond. Pure Appl. Chem. 2014, 86, 517–528.

(16) Fukuda, K.; Nagami, T.; Fujiyoshi, J.-Y.; Nakano, M. Interplay between Open-Shell Character, Aromaticity and Second Hyerpolarizabilities in Indenofluorenes. J. Phys. Chem. A 2015, 117, 10620–10627.

(17) Frederickson, C.D.; Rose, B.D.; Haley, M.M. Explorations of the Indenofluorenes and Expanded Quinoidal Analogues. Acc. Chem. Res. 2017, 50, 977−987.

(18) Frederickson, C.D.; Zakharov, L.N.; Haley, M. M. Modulating Paratropicity Strength in Diareno-Fused Antiaromatics. J. Am. Chem. Soc. 2016, 138, 16827−16838.

(19) Frederickson, C.K.; Barker, J.E.; Dressler, J.J.; Zhou, Z.; Hanks, E.R.; Bard, J.P.; Zakharov, L.N.; Petrukhina, M.A.; Haley, M. M. Synthesis and Characterization of a Fluorescent Dianthraceno­Indacene. Synlett 2018, 29, 2562–2566.

(20) Di Giovannantonio, M.; Urgel, J.I.; Beser, U.; Yakutovich, A.V.; Wilhelm, J.; Pignedoli, C.A.; Ruffieux, P.; Narita, A.; Müllen, K.; Fasel, R. On-Surface Synthesis of Indenofluorene Polymers by Oxidative Five-Membered Ring Formation. J. Am. Chem. Soc. 2018, 140, 3532−3536.

(21) Di Giovannantonio, M.; Eimre, K.; Yakutovich, A.V.; Chen, Q.; Mishra, S.; Urgel, J.I.; Pignedoli, C.A.; Ruffieux, P.; Müllen, K.; Narita, A.; Fasel, R. On-Surface Synthesis of Antiaromatic and Open-Shell Indeno[2,1-b]Fluorene Polymers and Their Lateral Fusion into Porous Ribbons. J. Am. Chem. Soc. 2019, 141, 12346−12354.

(22) Di Giovannantonio, M.; Chen, Q.; Urgel, J.I.; Ruffieux, P.; Pignedoli, C.A.; Müllen, K.; Narita, A.; Fasel, R. On-Surface Synthesis of Oligo(indenoindene). J. Am. Chem. Soc. 2020, 142, 12925–12929.

(23) Clair, S.; de Oteyza, D. G. Controlling a Chemical Coupling Reaction on a Surface: Tools and Strategies for On-Surface Synthesis. Chem. Rev. 2019, 119, 4717–4776.

(24) Wang, T.; Zhu, J. F. Confined On-Surface Organic Synthesis: Strategies and Mechanisms. Surf. Sci. Rep. 2019, 74, 97–140.

(25) Albrecht, F., Rey, D., Fatayer, S., Schulz, F., Pérez, D., Peña, D., Gross, L. Intramolecular Coupling of Terminal Alkynes by Atom Manipulation. Angew. Chem. Int. Ed. 2020, DOI: 10.1002/anie.202009200, and refs. therein.

(26) Cirera, B.; Giménez-Agulló, N.; Björk, J.; Martínez-Peña, F.; Martin-Jimenez, A.; Rodriguez-Fernandez, J.; Pizarro, A. M.; Otero, R.; Gallego, J. M.; Ballester, P.; Galan-Mascaros, J. R.; Ecija, D. Thermal Selectivity of Intermolecular versus Intramolecular Reactions on Surfaces, Nat. Commun. 2016, 7, 11002.

(27) Tran, B. V.; Pham, T. A.; Grunst, M.; Kivala, M.; Stohr, M. Surface-Confined [2+2] Cycloaddition towards One-Dimensional Polymers Featuring Cyclobutadiene Units. Nanoscale 2017, 9, 18305–18310.

(28) Di Giovannantonio, M.; Keerthi, A.; Urgel, J.; Baumgarten, M.; Feng, X.; Ruffieux, P.; Narita, A.; Fasel, R.; Müllen, K. On-Surface Dehydro-Diels–Alder Reaction of Dibromo-Bis(phenylethynyl)benzene. J. Am. Chem. Soc. 2020, 142, 1721–1725.

(29) The cycloaddition between a furane and a norbornyl-type dienophile attached through thiol groups to the STM tip and a gold surface, respectively, has been reported: Aragonès, A., Haworth, N. L.; Darwish, N.; Ciampi, S.; Bloomfield, N. J.; Wallace, G. G.; Diez-Perez, I.; Coote, M. L. Electrostatic Catalysis of a Diels–Alder Reaction. Nature 2016, 531, 88–91.

(30) Segura, J. L., Martín, N. o-Quinodimethanes: Efficient Intermediates in Organic Synthesis. Chem. Rev. 1999, 99, 3199–3146.

(31) Dinca, L. E.; Fu, C.; MacLeod, J. M.; Lipton-Duffin, J.; Brusso, J. L.; Szakacs, C. E.; Ma. D.; Perepichka, D. F.; Rosei, F. Unprecedented Transformation of Tetrathienoanthracene into Pentacene on Ni(111). ACS Nano 2013, 7, 1652–1657.

(32) Krüger, J.; García, F.; Eisenhut, F.; Skidin, D.; Alonso, J. M.; Guitián, E.; Pérez, D.; Cuniberti, G.; Moresco, F.; Peña, D. Decacene: On-Surface Generation. Angew. Chem. Int. Ed. 2017, 56, 11945–11948.

(33) Urgel, J. I.; Mishra, S.; Hayashi, H.; Wilhelm, J.; Pignedoli, C. A.; Di Giovannantionio, M.; Widmer, R.; Yamashita, M.; Hieda, N.; Ruffieux, P.; Yamada, H.; Fasel, R. On-Surface Light-Induced Generation of Higher Acenes and Elucidation of Their Open-Shell Character. Nat. Commun. 2019, 10, 861.

(34) Dorel, R.; McGonigal, P. R.; Echavarren, A. M. Hydroacenes Made Easy by Gold(I) Catalysis. Angew. Chem. Int. Ed. 2016, 55, 11120–11123.

(35) Zuzak, R.; Dorel, R.; Krawiec, M.; Such, B.; Kolmer, M.; Szymonski, M.; Echavarren, A. M.; Godlewski, S. Nonacene Generated by On-Surface Dehydrogenation. ACS Nano 2017, 11, 9321–9329.

(36) Colazzo, L.; Mohammed, M. S. G.; Dorel, R.; Nita, P.; García Fernández, C.; Abufager, P.; Lorente, N.; Echavarren, A. M.; de Oteyza, D. G. On-Surface Synthesis of Heptacene on Ag(001) from Brominated and Non-Brominated Tetrahydroheptacene Precursors. Chem. Commun. 2018, 54, 10260–10263.

(37) Diiodoterphenyl 8 was prepared by Suzuki coupling of 1,4-phenylenediboronic acid with 4-bromo-1-iodo-2-methylbenzene, followed lithiation with n-BuLi and treatment with I2. See Supporting Information for details.

(38) Obtained as a ca. 2:1 mixture with minor unsymmetrical isomer 11b. See Supporting Information for details.

(39) Zuzak, R.; Pozo, I.; Engelund, M.; Garcia-Lekue, A.; Vilas-Varela, M.; Alonso, J.M.; Szymonski, M.; Guitián, E.; Pérez, D.; Godlewski, S.; Peña, D. Synthesis and Reactivity of a Trigonal Porous Nanographene on a Gold Surface. Chem. Sci. 2019, 10, 10143–10148.

(40) Krejčí, O.; Hapala, P.; Ondráček, M.; Jelínek, P. Principles and Simulations of High-Resolution STM Imaging with a Flexible Tip Apex. Phys. Rev. B 2017, 95, 045407.

(41) Gross, L.; Mohn, F.; Moll, N.; Liljeroth, P.; Meyer, G. The Chemical Structure of a Molecule Resolved by Atomic Force Microscopy. Science 2009, 325, 1110-1114.

(42) Neaton, J.B.; Hybertsen, M.S.; Louie, S.G. Renormalization of Molecular Electronic Levels at Metal-Molecule Interfaces. Phys. Rev. Lett. 2006, 97, 216405.

(43) Horcas, I.; Fernández, R.; Gómez-Rodríguez, J.M.; Colchero, J.; Gómez-Herrero, J.; Baró, A.M. WSxM: A Software for Scanning Probe Microscopy and a Tool for Nanotechnology Rev. Sci. Instr. 2007, 78, 013705.

Table of Contents artwork